Appendix A Experimental evidence register

Table A1 identifies all 31 cited slab-experimental and field publications. Each row is a publication record; companion reports, mixed beam-and-slab studies, and field panels must not be summed as independent experiments. The stable R identifiers link this appendix to the spreadsheet. Publication-level coverage is complete for the cited corpus; numerical extraction is limited to source-traceable records.

Table A1. Cited slab-experimental and field publications and their database roles.

| ID | Source | Evidence subset | Counting or eligibility note |
| --- | --- | --- | --- |
| R002 | Abdul-Salam, B. (2014) | One-way shear | Doctoral thesis; experimental source. Potential overlap with Abdul-Salam et al. 2013 and 2016; thesis/journal counts must not be summed. |
| R003 | Abdul-Salam, B., Farghaly, A.S., & Benmokrane, B. (2016) | One-way shear | One-way slab experiments and mechanisms; potential thesis/conference overlap. |
| R004 | Abdul-Salam, B., Farghaly, A.S., Benmokrane, B. (2013) | One-way shear | CFRP one-way slab conference report; likely subset of 2014 thesis/2016 article. Specimen crosswalk required. |
| R010 | Aflakisamani, M., Mousa, S., Mohamed, H. M., Ahmed, E. A. et al. (2023) | Serviceability / punching | Full-scale GFRP lightweight SCC bridge-deck laboratory experiments; 2022 conference report in legacy workbook may duplicate. |
| R012 | Al-Sunna, R., Pilakoutas, K., Hajirasouliha, I. et al. (2012) | Deflection | Mixed program: 14 beams and 14 slabs, including steel controls. Slab subset: 12 FRP specimens and 2 steel controls. Published model ratios are series-level, not replicate-level. |
| R015 | Ali, Y. M. S., Wang, X., Guo, H., Liu, S., Li, D., Wu, Z. et al. (2024) | Static / fatigue | BFRP, steel and hybrid bridge-deck slab experiments; possible overlap with Ali 2023 static report in legacy workbook. |
| R018 | Alsunna, R. (2006) | Deflection | Thesis involving FRP flexural members; possible overlap with Al-Sunna 2012 mixed beam/slab article. |
| R022 | Benmokrane, B., El-Salakawy, E., El-Ragaby, A. et al. (2006) | Field / serviceability | Morristown Bridge field design and proof testing; failure strength not directly observed. |
| R023 | Berg, A. C., Bank, L. C., Oliva, M. G., & Russell, J. S. (2006) | Field / construction / cost | Wisconsin bridge construction and cost report; distinguish bar-reinforced deck from formwork system and cost assumptions. |
| R025 | Bouguerra, K., Ahmed, E. A., El-Gamal, S. et al. (2011) | Punching / CMA | Full-scale FRP bridge-deck tests; compare specimen IDs against El-Gamal program before pooling. |
| R027 | Carvelli, V., Pisani, M. A., & Poggi, C. (2010) | Fatigue / moving load | GFRP concrete deck slab fatigue experiments; inspect relation to 2006/other moving-load reports. |
| R034 | El-Gamal, S. (2005) | Punching / CMA | Thesis; potential overlap with El-Gamal et al. 2005 and other Sherbrooke laboratory papers. |
| R035 | El-Gamal, S., El-Salakawy, E., & Benmokrane, B. (2005) | Punching / CMA | Six full-scale deck slabs (3 GFRP, 2 CFRP, 1 steel) per source abstract; potential overlap with thesis. |
| R036 | El-Ragaby, A., & El-Salakawy, E. F. (2011) | Environmental-fatigue | Deck experiments under severe environmental and repeated-load conditions; independent programs/specimens need source-level audit. |
| R038 | El-Ragaby, A., El-Salakawy, E., & Benmokrane, B. (2003) | Wotton field | Primary Wotton Bridge report; proof/truck loading, not failure test. |
| R039 | El-Ragaby, A., El-Salakawy, E., & Benmokrane, B. (2007b) | Fatigue life | Primary GFRP deck fatigue experimental program; companion 2007a reuses evidence. |
| R040 | El-Salakawy, E., & Benmokrane, B. (2004) | Serviceability | Ten full-size one-way slabs 3100x1000x200 mm per ACI abstract; distinguish one-way test idealization from restrained two-way deck. |
| R041 | El-Salakawy, E., Benmokrane, B., El-Ragaby, A. et al. (2005) | Cookshire-Eaton field | Primary field bridge investigation; proof-load/service response. |
| R043 | El-Sayed, A., El-Salakawy, E., & Benmokrane, B. (2005b) | One-way shear | One-way FRP slab laboratory experiments. |
| R044 | Elgabbas, F., Ahmed, E., & Benmokrane, B. (2016) | Punching / CMA | Seven new full-scale specimens: six BFRP and one steel control. Earlier GFRP/CFRP specimens reproduced for comparison are not new tests. |
| R048 | Gao, C., Tauskela, L., & Fam, A. (2024) | Rolling / pulsating fatigue | Direct full-scale GFRP deck comparison under different fatigue loading paths. |
| R055 | Ju, M., Oh, H., & Sim, J. (2017) | Variable-amplitude fatigue | CFRP-reinforced deck slab cyclic experiments; distinguish tested variable amplitude from validated Miner law. |
| R058 | Mahroug, M., Ashour, A. F., & Lam, D. (2014) | Serviceability / continuous slabs | Continuous BFRP concrete slabs; generic slab laboratory evidence, not full bridge-system restraint. |
| R060 | Michaluk, C.R., Rizkalla, S.H., Tadros, G. et al. (1998) | One-way flexure | Eight one-way slabs with glass, carbon, or steel reinforcement. Reinforcement form and loading details must remain explicit. |
| R066 | Rossini, M., Cadenazzi, T., Nolan, S., & Nanni, A. (2019) | Halls River field | Field demonstration / construction report; no deck punching failure tests. |
| R073 | Zheng, Y., Sun, C., Deng, T., et al. (2014) | Punching / CMA | One-third-scale restrained GFRP deck experiments and arching model; same investigator group as 2012, independence must be reported cautiously. |
| R074 | Zheng, Y., Taylor, S. E., Zhou, L., Grattan, S., Sonebi, M. et al. (2024) | Thompson Bridge field | Six proof-loaded panels: four BFRP and two steel. All sustained 400 kN without failure. Separate from SCC simulation and lab programs. |
| R075 | Zheng, Y., Yu, G.Y., & Pan, Y. (2012) | Punching / CMA | GFRP deck laboratory experiments and ultimate-strength model; audit reuse in 2014 and numerical followups. |
| R077 | Zheng, Y., Zhou, L., Taylor, S.E., & Ma, H. (2019) | Serviceability | BFRP one-way serviceability program. Figure 6 program attribution recovered from the earlier author manuscript; exact specimen and concrete-matrix mapping unresolved. |
| R078 | Zheng, Y., Zhou, L.Z., Xia, L.P., et al. (2018) | Punching / CMA | SCC BFRP deck laboratory experiments; must not be merged with Thompson field proof panels. |
| R080 | Zhou, L., Dong, P., Zheng, Y., Song, G., & Wang, X. (2020) | Serviceability | GFRP one-way program with eleven slabs. Figure 6 program attribution recovered from the earlier author manuscript; exact specimen and concrete-matrix mapping unresolved. |

Database interpretation. A source may contribute to several response sections, but a specimen is counted once per declared analysis subset. Reported group ranges are not assigned to individual specimens. Repeated observations retain load or cycle context. Missing numerical values are not zero. Field proof loads and fatigue runouts are retained with a nonfailure flag and excluded from ordinary failure-load or fatigue-life regression.

Model assessment. The spreadsheet records whether a comparison has specimen-linked observations, source-reported predictions, independently reproducible inputs, or only a qualitative/graphical statement. Complete matched subsets support numerical ratios; incomplete figures support only bounded mechanism interpretation. Program-level external validation is separated from model calibration and subsequent tests by the same team.

Source overlap. Particular crosswalks requiring care include Abdul-Salam (2013, 2014, 2016), Alsunna (2006) and Al-Sunna et al. (2012), El-Gamal (2005) and associated journal reports, the two El-Ragaby et al. (2007) papers, and historical specimens reproduced in later deck-model comparisons. Numerical reanalyses and field companion publications add evidence, not new physical specimens.

El-Salakawy and Benmokrane (2004) and El-Sayed et al. (2005b) also require cross-publication reconciliation because their reported geometries and GFRP/CFRP populations are closely aligned. They are not automatically added as independent specimen populations.

Table A2. Source-reported service deflection ratios for FRP slab series in Al-Sunna et al. (2012), Table 5. Ratio = predicted/measured.

| Slab series | ACI 440.1R-06 | Eurocode 2 / Bischoff | Benmokrane et al. (1996) |
| --- | --- | --- | --- |
| SC1 | 1.08 | 0.73 | 1.13 |
| SC2 | 0.61 | 0.72 | 1.05 |
| SC3 | 0.71 | 0.81 | 1.13 |
| SG1 | 1.18 | 0.95 | 1.10 |
| SG2 | 0.66 | 0.92 | 1.24 |
| SG3 | 0.65 | 0.97 | 1.42 |

SC and SG identify CFRP and GFRP slab series. Ratios are published series-level summaries; they are not copied to each individual replicate. The service stage corresponds to the source's loading protocol, approximately 45% of estimated concrete strength at the compression face. All three model comparisons use the same six series. Ratios below one represent underprediction of deflection. Statistics in Section 3.2.2 are calculated from these rounded values.

Table A3. Source-reported punching ratios for BFRP slabs in Elgabbas et al. (2016), Table 3. Ratio = measured/predicted.

| Specimen | Edge restraint | CSA S806-12 | ACI 440.1R-06 |
| --- | --- | --- | --- |
| S2-B | Yes | 0.92 | 1.53 |
| S3-B | Yes | 1.13 | 1.86 |
| S4-B | Yes | 1.00 | 1.64 |
| S5-B | Yes | 1.06 | 1.67 |
| S6-B | Yes | 1.22 | 2.23 |
| S7-B | No | 0.93 | 1.69 |

Only S2-B to S6-B enter the five-specimen restrained summary; S7-B is reported separately. The steel control and previously published GFRP/CFRP comparison specimens reproduced in the source are excluded from this BFRP subset. Ratios below one indicate overprediction of measured resistance. Published rounded ratios permit an arithmetic check, but do not replace independent equation verification or code-scope qualification.